EECS 523 – Digital Integrated Circuit Technology

| SYLLABUS |  |
| --- | --- |
| LECTURE 1 |  |
| Topic |  |
|  | Introduction/Overview, Historical Review of Digital IC’s |
| Summary of Lecture Content |  |
|  | The class syllabus, schedule, prerequisites, materials, and general course guidelines are all discussed during this lecture. An overview of the history of digital IC’s is given. Technology has progressed from giant mechanical computers in 1834 that do not even have the capabilities of a modern four function calculator. The progression and timeline of bipolar, PMOS, NMOS, and CMOS transistors is introduced along with Moore’s Law. The transition from Small Scale Integration (SSI) to Very Large Scale Integration (VLSI) is discussed along with terms like submicron and deep submicron. These technologies have led us to circuit designs such as the Pentium 4 in 2002, which consists of 76 million transistors on an 11x11mm2 silicon wafer running at speeds in the 3 GHz range. |
| Supplementary Material |  |
|  | [Plummer01] Chapter 1: pages 3-4 |
| LECTURE 2 |  |
| Topic |  |
|  | Performance Metrics for Digital IC’s |
| Summary of Lecture Content |  |
|  | Digital technology performance can be compared by metrics in density, cost, reliability, speed, and power consumption. More density leads directly to more computational power and lower cost chips. Certain technologies are inherently denser, for instance NMOS is denser than CMOS. Design complexity, yield, packaging, and the number of processes or masks are a big portion of the cost of a technology. Reliability is diminished by hot carriers, latchup, oxide breakdown, and electron migration in today’s technologies. Digital designers are usually more concerned about power and speed metrics. An inverter with a capacitance load is used to calculate delay and switching power consumption for a technology. Speed is correlated to the propagation delay through a circuit. This delay can be thought of as the time it takes to charge and discharge a capacitance load, CL. Ring oscillators (chain of inverters) are also used to measure the speed of propagation for a given technology process. Power consumption has been the main factor in limiting technologies from being mainstream. Today this metric is even more important due to the increase in low power hand held devices. Power consumption is broken into static and dynamic power. Static power consists of DC power and leakage power. Dynamic power consists of the charging and discharging of the load capacitor and any short circuit power dissipation. |
| Supplementary Material |  |
|  | D.A. Hodges and H.G. Jackson, Analysis and Design of Digital Integrated Circuits, New York: McGraw-Hill, 1983. Chapter 4.3-6.6 |
| LECTURE 3 |  |
| Topic |  |
|  | Bipolar Digital Technology |
| Summary of Lecture Content |  |
|  | The Bipolar Junction Transistor (BJT) was the first widely successful digital logic family and an overview is given in this lecture. This technology has the advantage of being fast and low cost due to the limited number of masks needed. Unlike MOS technologies, the power-supply voltage for a bipolar transistor was kept constant (5V) as circuits were made smaller and denser. This made electrical breakdown a concern when the channel sizes were reduced significantly. Power and size considerations limited bipolar technology and gave way to lower power MOS technology for digital applications. Bipolar transistors remain important due to their characteristics for analog circuit applications, which include high gain and high-frequency performance. RTL, I2L, TTL, and ECL are just some of the chip interface technologies that utilize bipolar transistors. Schottky diodes are commonly used with these logic families to get ride of static charge buildup. |
| LECTURE 4 |  |
| Topic |  |
|  | MOS Digital Technology and Device Structure |
| Summary of Lecture Content |  |
|  | The Metal Oxide Semiconductor commonly referred to as MOS has been around since the 1960’s. PMOS was the first MOS technology that was widely produced and used only 4 masks. Enhancement mode NMOS devices couldn’t be produced at this time due to the large and quite variable oxide-charge densities. Depletion mode devices, opposite of enhancement mode, have an inversion layer present without any applied voltage. The threshold voltage is the most important physical feature of MOS devices. Threshold voltage (Vt) is equal to the work function difference between the gate and substrate minus the equilibrium potential, minus the static depletion region charge (QB/COX), and minus the oxide charge (QSS/COX). Vt is negative for PMOS and positive for NMOS enhancement mode devices. NMOS was desirable due to the mobility of an electron being much higher than that of a hole carrier. Many process changes aided in the transfer from using PMOS to that of NMOS. Cleanliness or clean rooms helped to prevent gate-oxide mobile ion charge. The move to using <100> Si instead of <111> Si limited the number of dangling bonds on the surface which controlled the oxide charge, Qss. Ion implantation was discovered as a method useful in adjusting the threshold voltage. Transition to poly-silicon gates was a large improvement in reliability over the aluminum gate because it allowed for self-alignment of the source and drain. This process improvement was possible due to the higher melting point of poly-silicon which allowed it to be deposited before high temperature steps. |
| Supplementary Material |  |
|  | [Wolf90] Section 5.3: The Evolution of MOS Technology |
| LECTURE 5 |  |
| Topic |  |
|  | CMOS Digital Technology and Device Structure |
| Summary of Lecture Content |  |
|  | Due to power consumption complementary MOS (CMOS) started to look like the most viable MOS solution. This lecture provides an introduction to CMOS technology. As NMOS designs grew in size or number of transistors, the static current also increased. The key to the success of CMOS is, if ignoring leakage currents, that CMOS consumes no power in the static state. The dynamic power dissipation of a CMOS inverter is given by CLVDD2f, where f is the switching frequency. CMOS is less dense, slower, and needs 11 masks as opposed to NMOS, which needs only 5. CMOS is also susceptible to latch-up, so guard rings and other isolation techniques need to be used. The input capacitance for a CMOS inverter is also higher, because it consists of 2 transistor gates per inverter. CMOS is currently a very cost effective and reliable solution. CMOS has much more resistance to temperature changes. Hot carrier degradation is less severe in a PMOS device then in NMOS, thus, CMOS has less degradation than NMOS. This is because CMOS doesn’t draw static current. CMOS is more resistant to electromigration because it has no static current therefore it has less interconnect failure due to this effect. Dynamic circuits and memory devices on the other hand are very susceptible to this effect. Power reduction allows for cheaper packaging, plastic versus ceramic. This also allows for cheaper system-wide cooling schemes. Overall, CMOS has become the most cost effective technology to manufacture today, coming at less than a 20% premium to NMOS. |
| Homework |  |
|  | Spectre (Cadence, Inc.) and Signal Scan (Cadence, Inc.) are used to review the concepts of power consumption and speed for CMOS and NMOS inverters. See Attachment: 523-HW1, and the miscellaneous material for this homework in the folder: 523-HW1-Files |
| Supplementary Material |  |
|  | [Wolf90] Chapter 6: CMOS Process Integration |
| LECTURE 6 |  |
| Topic |  |
|  | IC Fabrication: Diffusion |
| Summary of Lecture Content |  |
|  | The following two lectures provide a basic understanding of diffusion along with equations needed for calculating dopant diffusion profiles in silicon. Diffusion has historically been one of the most important processing steps used for integrated circuits. Diffusion is the movement of dopants within Si at high temperatures. One-dimensional diffusion follows Fick’s first law of diffusion, J = -D dN/dx. J represents the particle flux of the donor or acceptor impurity, N is the concentration of the impurity, and D is the diffusion coefficient. Fick’s 2nd Law states the rate of increase of concentration with time. The diffusion coefficient depends on the type of substrate, impurity atom type, and temperature. The diffusion coefficient can be calculated using D=Do*e^(-Ea/kT). Impurities can be delivered in a gaseous, liquid or solid form. Impurity atoms move through the silicon lattice via substitution or interstitial diffusion. Substitutional diffusion means that the impurity atom moves along vacancies in the lattice. Interstitial diffusion is when the impurity atom jumps from one interstitial site in the lattice to another. This method of diffusion is very fast and is hard to control in a fabrication environment. Impurity atoms can also replace the Si atom in the lattice and the Si atom would move into an interstitial site. |
| Textbook Reading |  |
|  | [Jaeger02] Chapter 4: Diffusion |
| Supplementary Material |  |
|  | [Plummer01] Chapter 7 (page 10): Intrinsic Dopant Diffusion Coefficients |
| LECTURE 7 |  |
| Topic |  |
|  | IC Fabrication: Diffusion (cont.) |
| Summary of Lecture Content |  |
|  | The diffusion process is usually done using two steps. First, predeposition is used to implant impurities in a shallow layer near the surface. The next step is a drive-in step to force impurities inside the silicon to a desired depth. Constant-source diffusion (predeposition) is when the impurity concentration is held constant at the surface. Under this condition N(x,t) = N0 erfc[x / 2(Dt)1/2], where N0 is the impurity concentration at the surface. Diffusion from a limited dose (drive-in) is called limited-source diffusion which is modeled using an impulse function. Fabrication typically brings the wafer through many time-temperature cycles. The combined effect of these steps can be determined by taking the sum of the Dt products to determine the final impurity distribution. For selective diffusion, SiO2 and Si3N4 can be used as a barrier layer. Lateral diffusion can be estimated at 80% of vertical or normal diffusion. Boron, Phosphorous and Arsenic are the most common dopants used. The pn junction produced by the implant can be calculated to be where the diffused impurity profile intersects the background concentration. Sheet resistance is useful for designers since it takes thickness into account. Therefore, a designer only needs a length and width to calculate resistance. The final method discussed in the lecture is gettering, which is a common technique used to remove unwanted impurities by attracting them to the surface. |
| Textbook Reading |  |
|  | [Jaeger02] Chapter 4: Diffusion |
| Supplementary Material |  |
|  | [Plummer01] Chapter 7 (page 10): Intrinsic Dopant Diffusion Coefficients |
| LECTURE 8 |  |
| Topic |  |
|  | IC Fabrication: Ion Implantation |
| Summary of Lecture Content |  |
|  | Ion implantation is another method for introducing dopants into Si and has many advantages over diffusion. Some of the key advantages are that ions move in a vacuum (cleaner process), it is a low temperature process, there is no lateral diffusion, and there is better control on the type and number of impurities for a given implant. An ion implanter is a particle accelerator that produces a high-velocity beam of impurity ions that can penetrate into the silicon. The impurity profile produced by ion implantation can be approximated by a Gaussian distribution function. This profile estimates the projected range along with the peak impurity concentration. The area under the impurity distribution curve is equal to the implanted dose if the implant is completely contained within the Si. The junction depth can be found at the depth at which the concentration equals the background concentration of the wafer or well. The two main process steps that use ion implantation are threshold voltage adjustment and well formation. Ion implantation does have some setbacks and limitations. For selective implantations there is a small amount of lateral diffusion. If the silicon lattice is oriented (7 degrees is common) the ions will tend to miss the silicon atoms and they will channel much deeper than the expected distribution. The curve we use for implantation generally assumes an amorphous surface which is not true for most Si substrates. The main issue with the high energy of implantation is that it damages the silicon lattice. Annealing or putting the silicon through a high temperature cycle will cause the lattice to reform. The negative effect of annealing is the extra diffusion (enhanced diffusion) that will occur. Rapid thermal annealing is now used. In this step the wafer is heated to 1300 degrees C for only seconds or milliseconds. This method for annealing allows ion implantation to be a very important process step in today’s IC fabrication. |
| Textbook Reading |  |
|  | [Jaeger02] Chapter 5: Ion Implantation |
| Homework |  |
|  | The homework deals with diffusion and ion implantation. See 523-HW2 |
| LECTURE 9 |  |
| Topic |  |
|  | IC Fabrication: Oxidation |
| Summary of Lecture Content |  |
|  | Silicon oxidizes when exposed to oxygen forming a layer of high-quality electrical insulator called silicon dioxide (SiO2). For fabrication this chemical reaction is called thermal oxidation. Oxide is easy to grow and creates an excellent barrier for selective impurity deposition. Oxidation can be modeled using Fick’s first law of diffusion that represents a particle flow per unit area or particle flux. For SiO2 the particle flux (J=D[NO-NI]/XOX) remains constant, meaning that the reactants do not accumulate in the oxide. The reaction rate equalsKSNI , where KS is the reaction rate constant at the oxide silicon interface. Thermal oxidation can be achieved by heating a Si wafer to a high temperature ( - 1200 degree C) in an atmosphere containing pure O2 or water vapor (H2O). The wet (H2O) oxidation is much faster than the more controllable dry (pure O2) method. The final thickness of an oxidation layer can be calculated using the initial thickness and time along with a linear (B/A) and parabolic (B) growth rate constant. These two constants depend on temperature and take the same form as the diffusion constant (D). Looking at a cross section of a growth region would show that 56% of the oxide grows out from the silicon surface and 44% grows into the Si surface. |
| Textbook Reading |  |
|  | [Jaeger02] Chapter 3: Thermal Oxidation of Silicon |
| LECTURE 10 |  |
| Topic |  |
|  | IC Fabrication: Oxidation (cont.) |
| Summary of Lecture Content |  |
|  | This lecture is a continuation from the previous lecture on thermal oxidation. Initially the growth rate is determined strictly by reaction rate at the Si surface and is said to be reaction limited. As oxide builds up the reactant must diffuse through the oxide to get to the Si surface to react and the reaction becomes diffusion limited. During oxidation, the impurity concentration at the interface can be increased or depleted depending on the dopant type and conditions. This is referred to as dopant redistribution. The segregation coefficient (m) is equal to the ratio of the concentration of the impurity in silicon to that of the impurity in the oxide. Boron is depleted from the silicon while phosphorous tends to pile up in Si at the oxide interface. Oxidation can be formed more rapidly if pressure is added to the gas system. The crystal orientation is also a factor in oxidation growth. Silicon <111> grows oxide much faster than <100> due to the number of dangling bonds on the surface. The impurity doping also has an effect on the oxidation rate. Very thin oxides can be produced by reducing temperature, using low pressure, diluting oxygen with other gases, using a vertical furnace, and by combining O2 and hydrogen gases for cleaner water vapor. In general the rate of oxide growth and necessary rate constants can be interpolated from graphs or charts for this class. |
| Textbook Reading |  |
|  | [Jaeger02] Chapter 3: Thermal Oxidation of Silicon |
| Homework |  |
|  | This homework assignment deals with different applications for the thermal oxidation properties presented in lecture and in the book. See Attachment: 523-HW3 |
| LECTURE 11 |  |
| Topic |  |
|  | IC Fabrication: Film Deposition |
| Summary of Lecture Content |  |
|  | In this lecture and the following lecture, many film deposition techniques are introduced. Fabrication requires many steps in which thin layers of various materials are deposited onto the surface of the wafer. Quality of the deposition can be effected by the material’s composition, contamination, defect density, and the electrical and mechanical properties such as resistivity and adhesion. Ideally the layer that is deposited is a uniform thickness over all surfaces whether they are vertical or horizontal. If the deposition has this uniformity it is said to have ideal conformity. The methods used to deposit materials can be broken up into two categories: Physical Vapor Deposition (PVD) and Chemical Vapor Deposition (CVD). Evaporation and sputtering are examples of PVD. Low pressure CVD and vapor-phase epitaxy are two methods used in CVD processes. Evaporation is one of the oldest methods used to deposit metals. The evaporation process takes place in a vacuum chamber for better control of film composition. The system will have a valve inlet to allow the evaporated metal to enter the chamber. The mean free path is an important material specific parameter that suggests whether the molecules will interact with background gases or if they will travel straight to the deposition target. Aluminum is used over gold and silver in evaporation because it makes a much better contact with silicon. Some of the advantages of evaporation is that it does little damage to the substrate and the film that is deposited is very pure due to the vacuum. Some of the disadvantages are that not all metals can be evaporated, poor step coverage, shadowing, and Al can dissolve into Si causing aluminum spiking. Today sputtering is more common and effective than evaporation. |
| Textbook Reading |  |
|  | [Jaeger02] Chapter 6: Film Deposition |
| LECTURE 12 |  |
| Topic |  |
|  | IC Fabrication: Film Deposition (cont.) |
| Summary of Lecture Content |  |
|  | Sputtering is a widely used physical deposition technique for metals. Sputtering works by bombarding the target metal with energetic inert gas ions. Atoms on the target are dislodged into free space and are then deposited onto the substrate. This method causes the particles to collide and go in multiple directions which can be referred to as Brownian movement. The mean free path of this method is much smaller than it is in evaporation, which provides much better step coverage. However, this method also has its disadvantages. The inert gas carrier, usually argon, can be implanted into the wafer. The substrate can heat up substantially which can cause non-uniformity across the wafer. The heat can also cause stress problems in the film because the film will shrink while the substrate cools. Chemical Vapor Deposition forms a thin film on the surface of a substrate by thermal decomposition of a gaseous compound. The CVD process involves many steps that take place in a reactor system at various temperatures and pressures. First the gas is transported to the deposition region. Then reactants are transported by diffusion from the main gas stream to the wafer surface. The reactants get absorbed by the wafer surface. Items migrate along the surface and react chemically to form films. These surface movements, based on temperature, determine the conformity of the film. Reaction by-products are disorbed into the main gas stream and are removed from the reaction chamber. The growth rate and mass transfer coefficient can be used to determine if the process will be mass transfer or reaction rate limited. Conformity can be worse if the process is mass transfer limited. Poly-silicon, silicon oxide, and silicon nitride are three key materials for IC fabrication that are deposited with CVD. |
| Textbook Reading |  |
|  | [Jaeger02] Chapter 6: Film Deposition |
| LECTURE 13 |  |
| Topic |  |
|  | IC Fabrication: Lithography, Wet and Dry Etching |
| Summary of Lecture Content |  |
|  | Photolithography is used to transfer patterns from masks to photoresist on the surface of a wafer. Ultraclean conditions are used to minimize defects caused by dust particles. The first step in this process is to clean the wafer. Next, a barrier layer such as silicon dioxide is formed. Photoresist then is applied to the surface of the wafer. To improve adhesion of the photoresist the wafer is heated for a short time, called soft baking. The mask for the desired layer is then aligned using computer controlled alignment systems. Following alignment, the photoresist is exposed through the mask with an ultraviolet light. A hard baking step is done to harden the photoresist and improve adhesion. Etching techniques are then used to etch away the window of photoresist and barrier that is detailed by the original mask. Wet chemical etching and dry plasma etching are the two options for the removal of material. The two relevant metrics for etching are anisotropy and selectivity. Anisotropy describes how many directions will etch at a time. An anisotropic etch only etches in one direction where as an isotropic etch will etch equally in all directions. Selectivity represents if an etch will etch unintended layers of material. Wet etching tends to etch under the edge of the mask, causing problems for small dimensions. Dry etching, however, can yield highly anisotropic etching. Physical sputtering, chemical plasma, and reactive ion are all methods of dry etching. Reactive ion etching is a physical and chemical etch that is widely used today. |
| Textbook Reading |  |
|  | [Jaeger02] Chapter 2: Lithography |
| LECTURE 14 |  |
| Topic |  |
|  | IC Fabrication: Shallow Trench Isolation (STI) |
| Summary of Lecture Content |  |
|  | Shallow trench insolation is used in deep submicron technologies to prevent degrading and destructive conditions such as latchup. A relatively shallow trench is etched in the substrate, and is then refilled with an insulator material. High temperature CVD is used to round the corners of the trench. The surface is planarized to complete the isolation structure. Both the NMOS and PMOS devices can be guarded by the STI oxide region. Silicon dioxide is commonly used and the trench is usually 10-20nm deep. Despite some difficulties with STI, it is becoming an acceptable replacement for the common LOCOS isolation commonly used today. Poly-buffered LOCOS is another option that is introduced during this lecture. |
| LECTURE 15 |  |
| Topic |  |
|  | Typical CMOS Process |
| Summary of Lecture Content |  |
|  | The next two lectures utilized chapter 2 from the supplementary material listed below (Plummer01) as a guide for a modern CMOS process flow. Each process step is discussed in detail using the cross-section pictures as a reference. The process described required 16 masks and more than 100 process steps. The cross-sections depict the basic CMOS inverter, which consists of a PMOS and NMOS transistor. This discussion provides a perspective on how individual technologies like oxidation and ion implantation are used. The substrate type and orientation is selected in the first step of this process. The wafer is then cleaned, followed by thermal oxidation. Nitride is deposited using LPCVD. Photoresist is then added along with a soft-bake. The first mask patterns the active areas and the nitride is etched off. Field oxide is grown using a LOCOS process. Boron is implanted to form the P-well for the NMOS devices. Phosphorus is implanted to form the N-well for this dual well technology. The wells are diffused to their final depths using a high temperature drive-in cycle. This is followed by two voltage threshold implants. These steps are pictured on pages 3-6 in the Plummer text. |
| Textbook Reading |  |
|  | [Jaeger02] Chapter 9: MOS Process Integration |
| Supplementary Material |  |
|  | [Plummer01] Chapter 2: CMOS Technology |
| LECTURE 16 |  |
| Topic |  |
|  | Typical CMOS Process (cont.) |
| Summary of Lecture Content |  |
|  | The CMOS process discussion continues based on the diagrams from pages 7-17 in the Plummer text. After the threshold voltage implant steps, a new thin oxide layer is grown on the silicon. Poly-silicon is deposited over the entire device and then etched off using an anisotropic dry etch. LDD regions are formed for the NMOS and PMOS devices using a low dose implant. Sidewall oxide spacers are added along the edges of the poly gates to minimize gate overlap issues and preserve the LDD implant regions. The main source and drain regions are then created using another implantation. These ion implantation steps are followed by a final high temperature step for annealing damage and for drive-in. The last process steps are for making contacts and adding metal layers. This begins with an oxide etch to allow for contacts to Si and Poly. Ti is deposited with sputtering and reacted with N2 to form TiSi2 and TiN. TiN is then etched to form local interconnects. Oxide is deposited using LPCVD followed by CMP planarization. Contact holes are etched and filled with metal. This is followed by another planarization step. Al is deposited by sputtering and then etched with plasma etching to form metal layer 1. Similar steps follow to form metal layer 2. Finally, a thick passivation layer of Si3N4 is deposited. |
| Supplementary Material |  |
|  | [Plummer01] Chapter 2: CMOS Technology |
| LECTURE 17 |  |
| Topic |  |
|  | Electrostatic Potential in MOS Structures |
| Summary of Lecture Content |  |
|  | Energy-band diagrams are used to illustrate surface potential in MOS structures in this lecture. The basic example is the MOS capacitor denoted as MOS-C. The energy-band diagram of the three components of the MOS-C are metal, silicon dioxide, and the silicon substrate. The band structures are all related to a common reference potential or vacuum level. The energy difference between the vacuum level and the Fermi level is called the work function. The MOS capacitor will charge until the Fermi levels line up causing the bands to bend. The flat band, accumulation, depletion, and inversion energy-band diagrams for p-type and n-type silicon are demonstrated in lecture. For an n-type device, MOS electrons build up on the Si surface in accumulation, and holes build up at the surface in inversion. The electrical field in the oxide is assumed to be constant, since there is usually no net charge in the oxide. The surface potential is explained based on doping concentration and temperature. The main point of this lecture is to give a background into the material needed for the calculation of threshold voltage in a MOS device. |
| Textbook Reading |  |
|  | [Wolf95] Section 3.3 |
| LECTURE 18 |  |
| Topic |  |
|  | Threshold Voltage |
| Summary of Lecture Content |  |
|  | The threshold voltage is a key parameter needed for MOS device characteristic calculations. This lecture describes the basic parameters used to solve for Vt. First, the depletion-layer width is defined as the distance to which the band bending extends. In the MOS case this width reaches a maximum value at the onset of strong inversion. Correlation is made in lecture between the MOS equation for width and the PN Junction depletion layer width. Energy band diagrams are used to look at the parameters necessary for calculating threshold voltage for a poly gate MOS device. The first parameter is the work function difference between the gate and substrate (MS), which is dependant on the doping of the poly gate. The next parameter is the equilibrium potential for a uniformly doped substrate (S), which is equal to two times the Fermi potential and is positive for PMOS and negative for NMOS. The static depletion region charge (QB) is dependant on the bulk doping concentration, Fermi potential, and the source to bulk voltage. The oxide charge per area at the oxide silicon interface (QSS) is assumed to have no value in today’s technology and is not controllable for threshold adjustment. The last term needed for threshold voltage calculation is the gate oxide capacitance per unit area (COX). The first two parameters (S and MS) are logarithmic with doping concentration and therefore can only have a little effect for threshold adjustment. COX needs to be kept large due to current drive and device size concerns. That leaves the static depletion region as the only parameter that can produce a significant change in the voltage threshold. The doping concentration can be changed using ion implantation to get the desired threshold voltage adjustment. |
| Textbook Reading |  |
|  | [Wolf95] Section 4.6 |
| LECTURE 19 |  |
| Topic |  |
|  | Implantation for Adjusting Threshold Voltage |
| Summary of Lecture Content |  |
|  | To the first order, if the implant and substrate are of the same type and the effective depth of the implant is less than the depletion max width, then the voltage threshold can be estimated using a box approximation. The box approximation and calculation of the threshold voltage after an adjustment implant is described for the rest of this lecture. There are three cases after approximating the threshold implant profile by using a step function. The first case is to approximate the VT change by considering the implant as a charged layer right at the Si-Si02 interface. This case is called the delta approximation. The second case uses a box estimate where the box does not cover the whole depletion region. VT is found in this case by finding the surface potential associated with the depletion region and then finding the voltage drop across the oxide. Case three assumes the implant is deeper than the max depletion region to begin with. The dose of the implant can be approximated. |
| Textbook Reading |  |
|  | [Wolf95] Section 5.8 |
| Homework |  |
|  | The homework deals with directional etching, and a complete 36 step CMOS process flow. See Attachment: 523-HW4 |
| LECTURE 20 |  |
| Topic |  |
|  | EXAM: MOS Devices and Technology |
| LECTURE 21 |  |
| Topic |  |
|  | Body Effect; Long Channel MOSFET |
| Summary of Lecture Content |  |
|  | Body effect refers to the effect of a source to substrate bulk voltage or body bias. This voltage increases the depletion region near the source. This effect can be factored into the original threshold voltage equation by using the body effect coefficient. The body bias can be altered with design intent or it can be an effect based on the stacking of transistors. This stacking effect can create a virtual voltage that causes a body effect shift in VT. For a MOSFET to have long channel properties the length of the depletion source plus the length of the depletion drain must be less than the effective length of the channel. This is usually true when the channel length is greater than 2µm. The directional fields Ey and Ex are introduced in lecture with a diagram similar to the one in Liu93. The Gradual Channel Approximation is described. Finally, the Square-Law model is derived. |
| Textbook Reading |  |
|  | [Wolf95] Section 5.1 |
| Homework |  |
|  | This homework gives a plot of the threshold voltage to an implant dose, the derivation for voltage and electric field in the y-direction for long-channel MOSFET theory, and a simple example showing how to use the Tsuprem4 process simulator. SEE attachment: 523-HW5, and 370-HW5-NMOS |
| LECTURE 22 |  |
| Topic |  |
|  | Sub-Threshold Current, Sub-Threshold Swing |
| Summary of Lecture Content |  |
|  | In this lecture, the sub-threshold characteristics of a MOSFET device are introduced. The subthreshold region immediately below the threshold voltage is also called the weak inversion region. The diffusion current density is used instead of the drift current density for this region. The equation for sub-threshold current (IDST) is derived. The subthreshold swing (St) is a parameter that will show how much leakage current exists. The swing is based on the inverse slope of the logarithm of device current versus the applied gate voltage. For low leakage, when the device is off you want the slope to be steep, and therefore desire a low swing value. Most devices achieve 70-120 mV/dec ID. St can be used to identify at what length short channel effects will appear. There is only a slight dependence on the bulk doping concentration, otherwise the subthreshold slope is rather insensitive to device parameters. Subthreshold swing is, however, directly dependant on temperature. |
| Textbook Reading |  |
|  | [Wolf95] Sections 5.2, 5.4 |
| LECTURE 23 |  |
| Topic |  |
|  | Short-Channel Effects |
| Summary of Lecture Content |  |
|  | The key motivation for the sub-micron MOSFET is higher density and speed. However, there are many issues that become apparent when moving below the 2 micron channel length boundary. Some of the leakage current issues include lowering of VT as channel length decreases, drain induced barrier lowering (DIBL) due to small channel length and large VDS, punchthrough, and an increase in isolation current. The reliability issues introduced with short-channel effects include gate oxide breakdown, hot carrier effects, and interconnect issues between devices. Mobility degradation, velocity saturation, and hot carriers account for about 95% of the important effects on a device. Drain and source resistance, inversion layer thickness, bulk charge as a function of channel potential, and a non-uniform channel doping profile are of minor importance to the overall short channel effects. The change in voltage threshold due to drain induced barrier lowering is derived in lecture based off of the Liu93 reference. The DIBL model is also compared against the charge sharing model in lecture. |
| Textbook Reading |  |
|  | [Wolf95] Section 5.4 |
| Homework |  |
|  | This homework compares the long channel model to the square law theory for current calculations. It also deals with the temperature dependency of threshold voltage and subthreshold swing, and the DIBL effect. See attachment 523-HW6 |
| Supplementary Material |  |
|  | [Liu93] p. 86-95 |
| LECTURE 24 |  |
| Topic |  |
|  | Short-Channel MOSFETS: A Unified IV Model |
| Summary of Lecture Content |  |
|  | The formulation of a Unified IV Model for short-channel MOSFETS is discussed in lecture. The first parameter that is introduced is mobility degradation. The Sabins, Clemens and the Liang equations for effective mobility are illustrated. Device current is derived using the new short channel effective mobility and velocity saturation. By manipulating this equation, it is easy to see how much the long channel MOSFET equation overestimates the device current. Also, if the length of a device is small but the oxide thickness continues to be thin relative to the length, then the device will share long-channel like behavior. |
| Textbook Reading |  |
|  | [Wolf95] Section 5.4 |
| Supplementary Material |  |
|  | [Liu93] pp. 86-95 |
| LECTURE 25 |  |
| Topic |  |
|  | Short-Channel Modeling Beyond Saturation |
| Summary of Lecture Content |  |
|  | Beyond saturation, the device current shift continues to grow more rapidly with an increase in applied voltage. This is different from the constant current seen for a long channel device diagram. The ideality factor (KI) is also introduced in this lecture. Devices with a KI of 50-60% is considered a good device. The concept of channel length modulation is introduced. The first method for finding delta of length is the Abrupt Junction Model, however this model is very elementary and not very useful. The second method that is described is the constant gradient field model. This model assumes electrons are moving in the delta length region at the saturation velocity. The last model is described in detail in the next lecture is called the pseudo 2-dimensional model. |
| Textbook Reading |  |
|  | [Wolf95] Section 5.5 |
| Supplementary Material |  |
|  | [Liu93] p. 86-95 |
| LECTURE 26 |  |
| Topic |  |
|  | Short-Channel Modeling: Pseudo 2-Dimensional Model |
| Summary of Lecture Content |  |
|  | The Pseudo 2-Dimensional model is used to calculate the velocity saturation region (VSR) length as a function of Vds-Vdsat. The model assumes that carriers in the VSR are velocity saturated (vsat), the electric field and voltage at the leading edge of the VSR are Esat and Vdsat, the drain is abrupt and perfectly conducting, and the current is confined to the junction depth of the drain. The model uses Gauss’s Law to solve for the quasi-Fermi level V(y’) and the electric field E(y’). This model is very good for VG greater than VD, which is usually the case in digital circuits. However, the model is not very good when VD is greater than VG because the electric field, Ey, doesn’t spread uniformly across the junction depth, xj. Finally, time is spent deriving equations for E(y’), Emax, and the delta length of the VSR using the pseudo 2-dimensional model. |
| Textbook Reading |  |
|  | [Wolf95] Section 5.5 |
| Homework |  |
|  | Problem #1 is based on short channel saturation current. Problem #2 deals with the vertical electric field equation. Problem #3 use long channel and short channel theory to determine the velocity of carriers at the source and drain. Problem #4 describes influence of certain parameters on current saturation level. See Attachment: 523-HW7 |
| Supplementary Material |  |
|  | [Liu93] p. 86-95 |
| LECTURE 27 |  |
| Topic |  |
|  | Hot Electron Effects |
| Summary of Lecture Content |  |
|  | Hot-Carrier effects can cause device failure and degradation in short channel devices. The two categories of effects introduced in lecture were hot carrier injection and cold carrier injection referred to as tunneling. In hot carrier injection the hole or electron must have enough inertia to jump over the SiO2 barrier layer. For electrons this barrier is 3.1eV. Higher electric fields near the drain produce energy greater than or equal to 1.5 eV. Tunneling is broken up into Fouler-Nordheim (FN) Tunneling and Direct Tunneling. Direct tunneling refers to carriers passing through the entire oxide band gap while FN tunneling refers to passing through only a partial thickness. The thin gate oxide is limited to about 3nm due to this effect. PMOS is less prone to hot carriers then NMOS due to a higher energy barrier and lower mobility. |
| Textbook Reading |  |
|  | [Wolf95] Section 7.3.1, 9.1 |
| Supplementary Material |  |
|  | [Hu89] Chapter 3 |
| LECTURE 28 |  |
| Topic |  |
|  | Hot Carrier Effects: Substrate and Gate Current |
| Summary of Lecture Content |  |
|  | Substrate current is one negative effect of hot carriers. ISUB goes through the low doped large resistance substrate which can lead to latchup. An analytical equation for ISUB is derived using the impact ionization coefficient. The coefficient shows how much impact ionization a carrier can have within an area. ISUB increases as the max E-field increases, which occurs as the channel length is reduced. Substrate current, ISUB, can cause a reverse body effect that reduces the threshold voltage and the depletion region. This effect is called the Substrate Current Induced Body Effect (SCBE). ISUB peaks at about 45% of VDD. Gate current (IGATE) arises from a sequence of events each with its own probability. Gate current requires the existence of hot electrons, a redirection collision, no collisions suffered in the Si before reaching the oxide, and no collisions to occur in the oxide and potential wells. The probability of an electron jumping into the gate oxide and the probability that the electron is attracted to the gate both factor into the calculation of IGATE. |
| Textbook Reading |  |
|  | [Wolf95] Section 7.3.1, 9.1 |
| Supplementary Material |  |
|  | [Hu89] Chapter 3 |
| LECTURE 29 |  |
| Topic |  |
|  | Hot Carrier-Induced Device Degradation |
| Summary of Lecture Content |  |
|  | Degradation of a device occurs over time due to hot carrier effects. The two main hot carrier defects include interface charge and oxide trap charge. Current drive decreases over time as the voltage threshold increases due to the oxide charges. In the lab, the change in threshold voltage or the change in sub-threshold swing can be used to measure degradation over time. Other effects include lower mobility and a reduced effective channel length, which can lead to punchthrough breakdown. Accelerated stress tests use ISUB calculations to estimate the average lifetime of a device. VDD can be set to produce the maximum ISUB to accelerate the testing. The lifetime of a device will depend on the application, however, 10 years is a good estimate for general calculations. |
| Textbook Reading |  |
|  | [Wolf95] Section 9.3-9.4 |
| Supplementary Material |  |
|  | [Hu89] Chapter 3 |
| LECTURE 30 |  |
| Topic |  |
|  | Techniques for Reducing Hot Carrier Degradation: DDD and LDD Devices |
| Summary of Lecture Content |  |
|  | The high lateral electric field is the main parameter that causes hot carrier degradation. Decreasing the voltage applied to the device is one way to reduce Em, however this will also degrade the performance of the device. Another technique is to reduce the density of trapping sites and interface states in the gate oxide by using special processing techniques. Removing hydrogen from the Si-SiO2 border will remove the effects of the interface charge. This is done by using another element such as Fluorine. Two other techniques include Double Doped Drain (DDD) and Lightly Doped Drain (LDD). These techniques are engineered to lower EM. The DDD process adds a little bit of phosphorus after the Arsenic drain implant. LDD uses an oxide spacer which allows for a low doped area for the drain under the gate. The LDD can be a harder process to implement due to the number of added fabrication steps that are required. |
| Textbook Reading |  |
|  | [Wolf95] Section 9.6 |
| Supplementary Material |  |
|  | [Hu89] Chapter 3 |
| LECTURE 31 |  |
| Topic |  |
|  | EXAM: focusing on lectures 21-30. |
| LECTURE 32 |  |
| Topic |  |
|  | Other Short-channel Effects: Series Resistance |
| Summary of Lecture Content |  |
|  | The degradation effect seen by series resistance is illustrated by adding a resistor between the source and gate (RS) and the gate and drain (RD). RS is the negative feedback element for this circuit and has more effect than RD. The equation for IDSAT and VDSAT are derived again with the addition of the series resistance parameter, RS. The voltage drop across these two resistors causes a small degradation in device current that can be seen on a ID-VDS graph. |
| LECTURE 33 |  |
| Topic |  |
|  | Other Short-channel Effects: Poly Gate Depletion Effect |
| Summary of Lecture Content |  |
|  | This lecture gives an overview of the material published by K. Chen’s dissertation on the Polysilicon Gate Depletion (PGD) Effect. The basis of this effect is illustrated using energy-band diagrams showing that the poly-silicon gate can also have a depletion region dependant on the doping concentration of the gate. This depletion region effectively lowers VGS seen at the oxide. This can also be illustrated as another capacitance (CDP) across the gate. This effect will slightly degrade the driving or current capabilities for a device at a given gate voltage. If VGS is small, the effect seen is also small. Increasing the doping concentration in the poly gate will cause less PGD effect. |
| Homework |  |
|  | Problem #1 deals with hot-carrier induced breakdown. Problem #2 deals with breakdown voltage. Problem #3 compares a non-LDD MOSFET to a MOSFET with an LDD structure. Problem #4 uses short channel theory to find device current. See attachment: 523-HW8 |
| Supplementary Material |  |
|  | K. Chen, Ph.D dissertation, p.31-37, 1998. Polysilicon Gate Depletion (PGD) Effect |
| LECTURE 34 |  |
| Topic |  |
|  | MOS Device Scaling Strategies |
| Summary of Lecture Content |  |
|  | As CMOS processes progress, physical features of the device must scale down accordingly. Many models are used to give an estimation of how to scale features together to get similar operation for a specific device. These scaling strategies are discussed. In general for scaling device width, length, thin oxide thickness, junction depths for source and drain, voltage, and threshold voltage all scale down while the doping concentration will scale up. Four of the main goals attributed to scaling that should hold true are that density, speed, and reliability will increase while power consumption will decrease. Constant field scaling and constant voltage scaling are discussed. Mixed or generalized scaling is also discussed. In industry, variations on these scaling strategies are used to match a specific process fabrication environment. More variations can be found in sections 5.6 and 5.7 in the Wolf95 textbook. |
| Textbook Reading |  |
|  | [Wolf95] Section 5.6, 5.7, 7.5 |
| Homework |  |
|  | Problem #1 is about scaling effects and PGD. Problem #2 is also based on scaling of technology. See attachment: 523-HW9 |
| Supplementary Material |  |
|  | Ping K. Ko, “Approaches to Scaling,” VLSI Electronics: Microstructure Science, vol. 18, chapter 1, 1989. ULSI Devices, Edited by C. Y. Chang and S. M. Sze, John Wiley & Sons, Inc., 2000. Chapter 5: SOI and Three-Dimensional Structures S. Thompson, P. Packan, and M. Bohr, “MOS Scaling: Transistor Challenges for the 21st Century,” Intel Technology Journal, Q3, p.1-19, 1998. |
| LECTURE 35 |  |
| Topic |  |
|  | Latch-Up |
| Summary of Lecture Content |  |
|  | Latchup is described using cross-section diagrams for a single and dual well CMOS process. Scaled CMOS technologies must be constructed to avoid latchup because breakdown is more probable in a smaller device. A back-to-back dual transistor diagram is used to explain the characteristics that will lead to latchup failure. The effects that induce latchup can be caused by avalanche breakdown of P/N junctions, photo generation leakage current caused by ionizing radiation, hot e- induced currents, voltage and current transients on power-up, inversion between the source and drain region of substrate MOS and well, and/or punch-through between substrate and source to drain region of a device. |
| Textbook Reading |  |
|  | [Wolf95] Sections 6.2, 6.4 |
| Supplementary Material |  |
|  | [Wolf90] Section 6.4: Latchup in CMOS |
| LECTURE 36 |  |
| Topic |  |
|  | Methods for Alleviating Latch-Up |
| Summary of Lecture Content |  |
|  | Techniques for reducing or eliminating latch-up include reducing the gain of the parasitic transistors with special processing techniques, reducing the parasitic resistances with special processing techniques, and by using layout procedures to decouple parasitic BJT’s. The gain can be lowered by physically separating the p+ (emitter) and p-well (collector) regions, however this will reduce circuit density. Other methods include trench isolation for devices to increase the distance carriers must travel, gold doping in substrate to produce trapping sites, neutron irradiation, and the use of retrograde wells. Process techniques that reduce parasitic resistance includes adding epitaxial layers on heavily doped substrate and again the use of retrograde wells. Processing techniques that decouple transistors include deep trench isolation with epi on a heavily doped substrate and silicon-on-insulator. Two circuit layout techniques for reducing latchup probability that can be used in conjunction with these processing techniques include adding numerous substrate and well contacts and the use of guard rings. |
| Textbook Reading |  |
|  | [Wolf95] Section 6.5 |
| Supplementary Material |  |
|  | [Wolf90] Section 6.4: Latchup in CMOS |
| LECTURE 37 |  |
| Topic |  |
|  | SIMOX and Other SOI Techniques |
| Summary of Lecture Content |  |
|  | Silicon on Insulator (SOI) is a fabrication technique that is good for eliminating the issue of latchup. The main reason SOI is latchup free is because the bulk silicon necessary for substrate current flow is eliminated. The bulk silicon is replaced by an insulator. There are many benefits of SOI, however, there are also many issues left to overcome. SOI technology is expensive and not all techniques are transferable from the current high yield fabrication techniques used for CMOS. Five methods for fabricating SOI technology are introduced. Silicon on sapphire (SOS) is a method in which silicon is grown on top of sapphire and LOCOS is used for insulation between devices. Recrystallization of polysilicon is a method that heats a thin layer of polysilicon, using a hot rod or laser, to recrystallize back to device grade silicon. The third method mentioned is Separation by Implanted Oxygen (SIMOX). This method uses high current ion implantation to imbed an insulation layer of silicon dioxide. The final two methods, Bond Etchback SOI and Smart Cut SOI, use etching or implanted hydrogen to remove layers of silicon to form a thin layer of the silicon lattice. In many of these techniques once the thin layer of silicon is created, most of the fabrication process and characteristic theory can be used with minor modifications. |
| Textbook Reading |  |
|  | [Jaeger02] Section 9.4 |
| Supplementary Material |  |
|  | Chang, Choi, Kedzierski, Lindert, Xuan, Boker, Hu, and King, “Moore’s Law Lives on,” IEEE Circuits & Devices Magazine, p.35-42, January 2003. |
| LECTURE 38 |  |
| Topic |  |
|  | SIMOX and Other SOI Techniques (cont.) |
| Summary of Lecture Content |  |
|  | Most of the equations introduced in this class for SOI technologies are relevant, however, a back gate effect needs to be introduced. Energy-band diagrams are used in lecture to show the back gate surface potential effect. Fully depleted, partially depleted, and accumulation mode devices are explained. The kink-effect in partially depleted devices happens because the body is left floating. The main benefits of SOI are that it eliminates latchup, is capable of higher speed due to smaller capacitance, has lower power consumption, has greater immunity to radiation effects because of the insulator, can lead to an increase in density, allows for 3-dimensional integration, reduces short channel effects, and has a smaller sub-threshold swing because of low body effect. |
| LECTURE 39 |  |
| Topic |  |
|  | Interconnect Resistive and Capacitive Parasitics; Performance Limitations |
| Summary of Lecture Content |  |
|  | The final lecture gives a short insight into the characteristics of interconnects. Interconnects can be broken into local and global interconnections. Diffusion and poly-silicon have a relatively high sheet resistance, which often restricts their use for interconnection. However, a silicide layer can be added to reduce the sheet resistance of these interconnects. The effective load of the wire due to mutual capacitance or coupling between wires is given in a brief example. Multiple layers of metal interconnection are used due to the density of the logic circuits. Global routing is a big concern as chips are getting larger in area while timing constraints and noise margins are getting smaller. |
| Textbook Reading |  |
|  | [Jaeger02] Chapter 7: Interconnections and Contacts |
| Supplementary Material |  |
|  | I.B. Dhaou, H. Tenhunen, and M. Ismail, “Modeling Techniques for Energy-Efficient System-on-a-Chip Signaling,” IEEE Circuits & Devices Magazine, p.8-17, January 2003. |
| LECTURE 40 |  |
| Topic |  |
|  | EXAM See attachment: 523-Exam3 |