ChE 393/469A

HOUR EXAM 2

Closed book and notes, 1 crib sheet.

(25 pts)	1. Qualitative questions

(4 pts)	a.	Give an advantage of rapid thermal processing over conventional furnace processing for use in process development.

(4 pts)	b.	Sketch what the size distribution looks like for silicon particles emerging from a fluidized bed CVD reactor, assuming the inlet particles all have the same radius rin.

(4 pts)	c.	List two varieties of gases held in the gas storage bunker in the basement of the UIUC Microelectronics Laboratory.

(4 pts)	d.	List two broad areas of research pursued in the Microelectronics Laboratory besides Si CMOS device processing.

(4 pts)	e.	Why does desorption from a surface typically have a much stronger temperature dependence than adsorption?

(5 pts)	f.	Sketch the physical setup for Czochralski growth of semiconductors.

(45 pts)	2.	Reactor loading

Suppose we have an LPCVD reactor for depositing selective epitaxial Ge operating under the following conditions:

gas in source line  = 	GeH4 at 2 x 10-3 torr in 1 x 10-1 torr helium

deposition rate  = 5 x 1016 atom/cm2min in a water batch of 25

flowrate vo   = 2 x 106 cm3/s		wafer diameter  = 30 cm

exposed wafer area for selective deposition  =  15% of front-side area

Tg = 325 K			     R = 6.26 x 104 torr⋅ cm3mol⋅K		1 mol = 6x1023 molecules

Suppose also that the reaction is limited by mass transport from the gas.

(Hint:  reactant is consumed, so the partial pressure of GeH4 deceases.)

(20)		a.	What is the percent reactant conversion with 25 wafers?

(20)		b.	What would be the percent conversion if we had to change the batch size to 50 wafers, changing nothing else?

(5)		c.	What would be the corresponding growth rate?

(30 pts)	3.	In one of the steps needed to nucleate TiSi2 selectively on Si vs SiO2 before doing CVD, an etching step with a chlorinated species is needed to take TiSi2 nuclei off the oxide.  The kinetics of this etching are controlled by the removal of Ti as TiCl4.

Kinetic parameters appear below:

| Adsorption of Cl2 | Desorption of TiCl4 |
| --- | --- |
| S=So 1−θCl | novo=1x108s-1 |
| So=0.5 | Ed=0.83 eV=19.2 kcal/mol |
| no=8x1014 molec/cm2 | N(order) in nCl=2 |
| M (molecular weight)=70 |  |

Note:		gas flux at surface:  fmoleccm2⋅s	=4x1020300Tg28M12Ptorr

R	=	1.987 cal/mol  K

Assuming the gas temperature Tg is 27oC and PCl2=5 x 10-3 torr, calculate the

chlorine coverage θCl at a surface temperature T of 450oC.

(30 pt Grad)	4. 	This problem is for students taking ChBE 469A only.  Do not answer if you are taking ChBE 393.

On occasion, chlorinated species are used to thermally etch silicon for microelectronics fabrication.  Etching of silicon by HCl occurs through the following overall heterogeneous reaction:

Si(s) + 2HCl(g) → SiCl2(g) + H2(g)

The following rate expressions have been measured in the EGS laboratory and elsewhere for the individual steps:

(1)	Adsorption of HCl

SHCl=0.1 1−θC1−θH

Incident flux (molec/cm2s) = k1P = 3.37x1020P (torr)

So let rl (monolayers/s) = Sk1P/no=Sok1Pno1−θCl−θH≡KA1−θCl−θH

where no = 6.8x1014 molec/cm2.

(2)	Desorption of SiCl2

r2 (monolayers/s)	=	k2θCl2=ν2 exp −E2/RT θCl2

where			ν2=4x1016s−1

E2 = 72000 cal/mol.

(3)	Desorption of H2

r3 (monolayers/s)	=	k3θH=ν3 exp −E3/RT θH

where			ν3=6x1013s−1

E3 = 51000 cal/mol.

The object here is to develop a predictive model for the Si etch rate as a function of the controllable system variables PHCl and T.

(8 pts)	(a)	Write steady-state mass balances for each atomic species in terms of r1, r2, r3, and the Si etch rate rE.

(8 pts)	(b)	Use these equations together with the individual rate expressions given above to find θCl in terms of KA, k2, and k3.  Be sure to pick the appropriate root of the quadratic equation you encounter.

(7 pts)	(c)	Derive an expression for rE in terms of the quantities k2, (k2/KA) and (KA/k3) only.

(7 pts)	(d)	Use this expression to show that rE becomes independent of PHCl as this pressure becomes very large.  At 500oC (a typical processing temperature), how large does PHCl have to be to reach this limit?