ChE 393/469A

Homework 4

(15 pts)	1. 	If one assumes Langmuir adsorption:

-	single kind of binding site

-	noninteracting adsorbate, one per site

-	no dissociation

one can derive:	S = So (1-θ)		where θ≡nno

const

0≤θ≤1

no=sa {t'n density1015moleccm2

(5)	a.	Assuming no desorption or reaction, write the differential equation needed to obtain θt in terms of P, t, and any other variables you may need.

(10)	b.	Assuming θ0=0, solve the differential equation to derive an expression for the time dependence of θ.

a particular crystal orientation

(20 pts)	2.	H2 adsorbs dissociatively on Si(111) according to the following kinetics:

Adsorption			    Desorption

S = 0.16 (1-θ)2		N = 2 (order)

no = 8 x 1014 atom/cm2		υd=91 cm2 molec s

m = 3.3 x 10-24g (mass)		Ed = 62 kcal/mol

kB = 1.38 x 10-16 erg/K		R = 1.987 cal/molK

1 torr = 1330 dyne/cm2

This adsorption system is important in several forms of CVD where H2 is the carrier gas for the reactive precursor.

(10)	a.	Assuming Tg = 300 K, Tsurf = 1000 K (a typical processing temperature), and adsorption-desorption equilibrium with no surface reaction develop a numerical expression relating θ to P(Torr).

(10)	b.	Below what P does θ begin to drop significantly below unity?